## Slide 2: Outline

## Slide 3: Carbon nanotubes can be visualized as rolled up sheets of graphene.

## Slide 4: While there are many different types of nanotube structures, this thesis focuses solely on single-wall carbon nanotubes (SWCNTs).

## Slide 5: For 3-D materials, the Sommerfeld factor enhances interband absorption.

## Slide 6: However, for 1-D materials, the Sommerfeld factor suppresses optical absorption of interband states.

## Slide 7: Exciton binding energies in SWCNTs can be on the order of hundreds of meV.
Show binding energies of SWCNTs

## Slide 8: In the past, sample preparation techniques were only capable of making SWCNT suspensiosn with many different chiralities.

## Slide 10: However, modern techniques have made single-chirality enriched samples more accessible.

## Slide 11: Screening of Coulomb interactions in SWCNTs by an external dielectric can affect bang gap renormalization and the binding energies of excitons.

## Slide 12: As a result of the screening induced by the external dielectric, optical resonances can redshift as the dielectric constant increases.

## Slide 13: For both samples, the SWCNTs were suspended using either the polymer PFO-Bpy or the surfactant sodium deoxycholate.

## Slide 14: Schematic Diagram of the Experimental Apparatus
Laser
Neutral
Density Filter
Sapphire
Sample
Optical Parametric Amplifier
Delay
Stage
Lens
Wavelength
Separator
Optical Fiber
Spectrometer
Optical Shutter
White Light
Continuum

## Slide 15: Slide showing what I’m going to talk about in next two slides

## Slide 16: Ultrafast all-optical switching devices harness nonlinear optical phenomena as a switch mechanism.

## Slide 17: The optical Stark effect can be utilized in the designs of optical switching devices.
Optical
Pump

## Slide 18: We observed a clear signature of the optical Stark effect in (6,5) SWCNTs.

## Slide 19: A coherent blueshift of the E11 resonance occurred. We also observed a residual signal due to the creation of excitons via multi-photon processes.

## Slide 20: Two ways to describe the dephasing dynamics of the system include a phenomenological model and a quantum-kinetic approach that involves quantum memory.

## Slide 21: The simulations including quantum memory best reproduced our data.

## Slide 22: The observed blueshift appropriately scales with the intensity of the optical pump.

## Slide 23: In resonantly exciting the E11 resonance, we observed spectral ringing due to interference between the pump and probe photons.

## Slide 24: Transition/Summary Slide

## Slide 25: Desire to make other optoelectronic devices like lasers. Is population inversion possible?

## Slide 26: Slide on Exciton Mott Transition

## Slide 27: This was first investigated by Ostojic et al who were not able to observe quenching of excitonic resonances in their SWCNT suspension.

## Slide 28: Slide on what is exciton-exciton annihilation

## Slide 29: This in some ways is related to other questions regarding the rate at which exciton-exciton annihilation occurs.

## Slide 30: Slide showing where we pumped and where we probed the samples.

## Slide 45: Summary